## Slide 1
MIL-PRF-32662: Operationalizing Science through Anticipatory/Translational DOD Performance Requirements
Robert Jensen
DEVCOM ARL
18 MAY 2022
DEVCOM ARL
A
Robert Jensen, 240-676-9401
U.S. Army
Notes: Version 05.26.2022

## Slide 2: MIL-PRF-32662: Adhesive, High-Loading Rate, for Structural and Armor Applications
Army capability gaps & commercial opportunity
Leap-ahead performance motivated by Ground Vehicle armor
Translational science
Anticipatory timing
Data science enabled
August 2020

## Slide 3: 2 Problems
Army capability gap
  High strength & high damage tolerance adhesives for bonded armor
Pain points
  Understanding & translating high-strain rate and non-linear fracture mechanics into relevant product metrics
  Ambiguous operating environment with rapid evolution pace
Traditional solution
  Peer review academic studies, publications & conference presentations
    Low impact & low commercial relevance
Adhesives industry challenges
  Market penetration with new product
Pain points
  New product qualification for customers is labor intensive and expensive
    Incumbent lock-in
Traditional solution
  Free product samples & PDF technical data sheets
    Relying on customer validation of performance
    Low success rate
Notes: Redman, T.C., 2016. Bad data costs the US $3 trillion per year. Harvard Business Review, 22, pp.11-18. https://hbr.org/2016/09/bad-data-costs-the-u-s-3-trillion-per-year

## Slide 4: 2 Problems made for each other
Army capability gap
  High strength & high damage tolerance adhesives for bonded armor
Pain points
  Understanding & translating high-strain rate and non-linear fracture mechanics into relevant product metrics
  Ambiguous operating environment with rapid evolution pace
Traditional solution
  Peer review academic studies, publications & conference presentations
    Low impact & low commercial relevance
Adhesives industry challenges
  Market penetration with new product
Pain points
  New product qualification for customers is labor intensive and expensive
    Incumbent lock-in
Traditional solution
  Free product samples & PDF technical data sheets
    Reliant on customer validation
    Low success rate
2 intractable problems if viewed independently
Solvable when paired together
Notes: R. Jensen, W. Kosik, J. Gardner, D. O’Brien. “Critical adhesive needs for Army applications and opportunities for innovation,” ARL-RP-323, June 2011
R. Jensen, W. Kosik Chaney, D. DeSchepper, D. Flanagan. “Leveraging Army unique mission requirements to advance the state-of-the-art in adhesives development,” ARL-RP-360, March 2012.

## Slide 5: Army capability gaps & commercial opportunity
projectile
backing plate
ceramic strike face
adhesive
$$$, complex,
commercially irrelevant
¢¢¢, “simple”,
commercial benchmark
Notes: ASTM Standard D1002-10 "Standard Test Method for Apparent Shear Strength of Single-Lap-Joint Adhesively Bonded Metal Specimens by Tension Loading (Metal-to-Metal)." ASTM International, West Conshohocken, PA, 2010, DOI: 10.1520/D1002-10, www.astm.org
Gao et al. Influence of epoxy adhesive layer on impact performance of TiB2-B4C composites armor backed by aluminum plate. International Journal of Impact Engineering 122, 60-72 (2018).
Bogetti et al. Predicting the nonlinear response and failure of composite laminates: Correlation with experimental results. Composites Science and Technology 64, 477-485 (2004).
Bartus. A review: Impact damage of composite materials. Journal of Advanced Materials 39, 3-21 (2007).
Bogetti et al. Predicting the nonlinear response and failure of composite laminates: Correlation with experimental results. Composites Science and Technology 64, 477-485 (2004).
“Collaborative Research Alliance (CRA) for Materials in Extreme Dynamic Environments (MEDE)”, funding opportunity title announced by the U.S. Army Research Laboratory, 2011, http://www.arl.army.mil/www/pages/532/FINAL_MEDE_PA.pdf

## Slide 6: Army capability gaps & commercial opportunity
Max strength (MPa)
High strength & very stiff
Variable strength & high damage tolerance

## Slide 7: Army capability gaps & commercial opportunity
Max Strength (MPa)
Max strength (MPa)
Correlation statistics
Max strength (MPa)
Notes: J. Robinette, J. Gardner, R. Jensen, S. McKnight. “Lap-shear strength versus elongation to failure of candidate composite armor adhesives,” ARL-TR-4862, June 2009.
R. Jensen, W. Kosik Chaney, J. Kaufman, B. Henrie. “Screening adhesively bonded single-lap-joint testing results using nonlinear calculation parameters,” ARL-RP-362, March 2012.
R. Jensen, D. DeSchepper, D. Flanagan. “Multivariate Analysis of High Through-Put Adhesively Bonded Single Lap Joints: Experimental and Workflow Protocols,” ARL-TR-7966, June 2016. http://hdl.handle.net/11256/699
R. Jensen, D. DeSchepper, D. Flanagan “Multivariate analysis of high through-put adhesively bonded single lap joints”, International Journal of Adhesion and Adhesives, 89, 2019, 1-10.

## Slide 8: Army capability gaps & commercial opportunity
Max strength (MPa)
Displacement at complete failure (mm)
Including total joint yielding!!!
High damage tolerance
Poor damage tolerance
projectile
backing plate
ceramic strike face
adhesive

## Slide 9: Army capability gaps & commercial opportunity
Max strength (MPa)
Displacement at complete failure (mm)
Army capability gap

## Slide 10: Army capability gaps & commercial opportunity
Max strength (MPa)
Displacement at complete failure (mm)
Commercial opportunity

## Slide 11: Army capability gaps & commercial opportunity
Max Strength (MPa)
Displacement at complete failure (mm)
Group I
Strength ³ 10.0 MPa
displacement > 3.81 mm
Group III
Group II
Group IV
MIL-PRF-32662: Adhesive, High-Loading Rate, for Structural and Armor Applications
Minimal test burden, optimized for armor
  Single lap joint
    Room temp
    Hot/wet
    Elevated temp
  Mode I stress corrosion cracking
  Pre-2018 all Group I adhesives were experimental and failed environmental conditioning
Notes: R. Jensen, D. DeSchepper, D. Flanagan, W. Kosik-Chaney, J. Robinette, G. Chaney, C. Pergantis. “Adhesives: test method, groups assignment, and categorization guide for high-loading rate applications,” ARL-ADHES-QA-001.00 rev 1.0, ARL-SR-288, June 2014.
R. Jensen, D. DeSchepper, D. Flanagan, G. Chaney, C. Pergantis. “Adhesives: Test Method, Group Assignment, and Categorization Guide for High-Loading-Rate Applications – Preparation and Testing of Single Lap Joints,” ARL-ADHES-QA-001.01 Rev 2.2, ARL SR-0356, April 2016.
Strategic Environmental Research and Development Program, “Understanding Corrosion Protection Requirements for Adhesive Bond Primers”, SERDP-WP-2144, September 2016.
R. Jensen, D. Flanagan, D. DeSchepper, C. Pergantis. “Adhesives: Test Method, Group Assignment, and Categorization Guide for High-Loading-Rate Applications – History and Rationale,” ARL-ADHES-QA-001.01 Rev 2.2, ARL SR-0371, April 2017.
R. Jensen, D. Flanagan, D. DeSchepper, M. Silton. “Single-Lap-Joint Screening of Hysol EA 9309NA Epoxy Adhesive,” ARL-TR-8011, May 2017. http://hdl.handle.net/11256/939
MIL-STD-3059 (MR). Acceptance criteria for adhesives for high-loading rate applications, Department of Defense Test Method Standard, 22 November 2018.
MIL-PRF-32662, Performance Specification, “Adhesive, High-Loading Rate, for Structural and Armor Applications”, 13 August 2020.
B. Rindespacher, B. Placzankis, W. Lum, R. Jensen. “MIL-PRF-32662: Adhesive, High-Loading Rate, for Structural and Armor Applications— Frequently Asked Questions”, ARL-TN-1035, September 2020.

## Slide 12: Leap-ahead performance motivated by Ground Vehicle armor
Max Strength (MPa)
Displacement at complete failure (mm)
PPG PR-2930
  Toughened epoxy
  Passed environmental tests
  Commercially scaled
Group I
Notes: PPG Development of PR-2930: Research was sponsored by the Army Research Laboratory and was accomplished under Cooperative Agreement Number W911NF-13-2-0046 to Drexel University and Sub-agreement to PPG Industries, Inc. The views and conclusions contained in this document are those of the authors and should not be interpreted as representing the official policies, either expressed or implied, of the Army Research Laboratory or the U.S. Government. The U.S. Government is authorized to reproduce and distribute reprints for Government purposes notwithstanding and copyright notification herein.

## Slide 13: Leap-ahead performance motivated by Ground Vehicle armor
15% of $1.5B/year vehicle assembly market*
Growth rate at 4X GDP
MIL-PRF-32662
Embedded drivers for armor bonding
Outcomes
TRL1 to MRL9 in 4 years
Independent validation of MIL-PRF-32662’s data-driven ballistic to static correlations
1st place 2020 industry innovation award
Available for DoD trials as obtainable commercial product
* “Breakthrough to a World Challenge, BETAMATE Structural Adhesives", Dow Automotive Systems
3m.com
Notes: https://www.ascouncil.org/page/Innovation_Awards#:~:text=The%20ASC%20Innovation%20Awards%20Program,needs%20and%20advancements%20in%20technology.

## Slide 14: Leap-ahead performance motivated by Ground Vehicle armor
Max Strength (MPa)
Displacement at complete failure (mm)
PPG PR-2930
  Toughened epoxy
  Mode I Fracture Energy (GIC) 3,200 +/- 450 J/m2
  Aerospace 1,000 – 2500 J/m2
Group I
Notes: F. Palmieri et al “Optimized surface treatment of aerospace composites using a picosecond laser”, Composites Part B, 175, 2019, 107155.

## Slide 15: Leap-ahead performance motivated by Ground Vehicle armor
Max Strength (MPa)
Displacement at complete failure (mm)
Validated ballistic tolerance
Group I
Bondline survived intact
Notes: Ballistic images cleared for public release by Natick SC April 2021.

## Slide 16: Translational science
Bohr
Edison
Pasteur
Tinkering
Fundamental understanding
Relevance
Peer review papers
Performance requirements
MIL-PRF-32662
Basic research
Applied research
Use-inspired basic research
Notes: Donald Stokes Pasteur’s Quadrant, Basic Science and Technological Innovation, Brookings Institution Press, 1997

## Slide 17: Anticipatory timing
Performance
Time
Anticipatory standards
Enabling standards
Responsive standards
Egyedi and Sherif. Standards dynamics through an innovation lens: Next-generation Ethernet networks. IEEE Communications Magazine 48, 166-171 (2010).
Existing technology
Quality assurance
Forward looking
Minimal guidance
MIL-PRF-32662
Platform development
Reduced cost
Telecommunications
MMM-A-132
MIL-PRF-?????
Notes: MIL-PRF-32662 “Adhesive, High-Loading Rate, for Structural and Armor Applications”
  Lap shear strength
    RT
    Hot/wet
    1600F
  Crack extension test
    Salt/fog
  New product developed in 2018, anticipated qualifications in 2022
MMM-A-132 “Adhesives, Heat Resistant, Airframe Structural, Metal to Metal”
  MMM-A-132, origin date – 1950’s
  MMM-A-132A, origin date – 24 August 1981
  MMM-A-132B, origin date – 1 April 1994
  Inactivated – 19 April 2001
  Reactivated – 14 February 2005
  Notice of validation for acquisition – 05 September 2019
  QPD actively maintained by DoD
Test Matrix
  Tensile shear (9 temperature, time, and fluid immersion variations)
  T-peel
  Blister detection
  Creep rupture (4 temperature variations)
Product qualifications
  20 adhesive qualified from 1954-1969
  Current Cytec product qualified in 1980 and 1989, then updated and re-qualified in 2020 and 2022
AMS-A-25463 “Adhesive, Film Form Metallic Sandwich Construction”
  MIL-A-25463, origin date – 1950’s
  Amendment 2, 1961
  Revision A - 1971
  Revision B - 1982
  AMS-A-25463, 1999 – reaffirmed 2013
  QPD actively maintained by DoD
Test Matrix
  Sandwich peel strength (RT)
    1800F
    -670F
  Flatwise tensile strength (RT)
      1800F or 3000F or 5000F
      -670F
  Flex strength (RT)
      1800F or 3000F or 5000F
      -670F
  Flex strength after 192 hours (hot)
  Creep deflection, 192 hours (RT)
  Creep deflection, 192 hours (hot)
  Flex strength (hot/wet)
  Flex strength (JP-4)
  Last product qualified in 1973

## Slide 18: Data science enabled
Correlation statistics
Relational database
Data pedigree
Data integrity
Digital infrastructure
Notes: D. DeSchepper, D. Flanagan, E. Elburn, R. Jensen, B. Henrie, P. Wimberley. “Support and development of workflow protocols for high throughput single-lap-joint testing – data management,” ARL-RP-426, April 2013.
D. Flanagan, D. DeSchepper, E. Elburn, R. Jensen. “Support and development of workflow protocols for high throughput single-lap-joint testing – experimental,” ARL-RP-425, April 2013.

## Slide 19: Data science enabled
Commercial applications
Non-DOD sales
Self-qualified vendor data
MIL-PRF-32662
Notes: D. DeSchepper, D. Flanagan, E. Elburn, R. Jensen, B. Henrie, P. Wimberley. “Support and development of workflow protocols for high throughput single-lap-joint testing – data management,” ARL-RP-426, April 2013.
D. Flanagan, D. DeSchepper, E. Elburn, R. Jensen. “Support and development of workflow protocols for high throughput single-lap-joint testing – experimental,” ARL-RP-425, April 2013.

## Slide 20: Data science enabled
WPI Cooperative Agreement W911NF-19-2-0112
Open system
Dual-use
Digital
platform
Closed system
Vendor
DoD
Vendor
DoD
Traditional spec
MIL-PRF-32662
Materials Experiments
Database Management
Data Visualization
Pattern Recognition
Model Validation
New Inventions

## Slide 21: MIL-PRF-32662: Adhesive, High-Loading Rate, for Structural and Armor Applications
Army capability gaps & commercial opportunity
Leap-ahead performance motivated by Ground Vehicle armor
Translational science
Anticipatory timing
Data science enabled
August 2020